## Slide 1: Saturated soil modelling: Griffith University: February 2010
Elastic modelling
David Muir Wood
d.muirwood@dundee.ac.uk

## Slide 2
Elasticity
Hooke's law
elastic behaviour in triaxial compression: drained/undrained
measurement of elastic properties with different devices
elastic anisotropy
elastic nonlinearity - hyperelasticity

## Slide 4
To fill the vacancy of the ensuing page, I have here added a decimate of the centesme of the Inventions I intend to publish, though possibly not in the same order, but as I can get opportunity and leasure; most of which, I hope, will be as useful to Mankind as they are yet unknown and new.
2. The true Mathematical and Mechanichal form of all manner of Arches for Building, with the true butment necessary to each of them. A Problem which no Architectonick Writer hath ever yet attempted, much less performed.
abcccddeeeeefggiiiiiiiillmmmmnnnnnooprrsssttttttuuuuuuuux.
3. The true Theory of Elasticity or Springiness, and a particular Explication thereof in several Subjects in which it is to be found: And the way of computing the velocity of Bodies moved by them.
ceiiinosssttuu
Hooke’s law
A description of helioscopes and some other instruments. London 1676.

## Slide 5
To fill the vacancy of the ensuing page, I have here added a decimate of the centesme of the Inventions I intend to publish, though possibly not in the same order, but as I can get opportunity and leasure; most of which, I hope, will be as useful to Mankind as they are yet unknown and new.
2. The true Mathematical and Mechanichal form of all manner of Arches for Building, with the true butment necessary to each of them. A Problem which no Architectonick Writer hath ever yet attempted, much less performed.
abcccddeeeeefggiiiiiiiillmmmmnnnnnooprrsssttttttuuuuuuuux.
Ut pendet continuum flexile, sic stabit contiguum rigidum inversum.
(As hangs the flexible chain, so, inverted, stands the rigid arch.)
Hooke’s law

## Slide 6
Ut pendet continuum flexile, sic stabit contiguum rigidum inversum.
(As hangs the flexible chain, so, inverted, stands the rigid arch.)
St Peter’s: Poleni: 1748

## Slide 7
To fill the vacancy of the ensuing page, I have here added a decimate of the centesme of the Inventions I intend to publish, though possibly not in the same order, but as I can get opportunity and leasure; most of which, I hope, will be as useful to Mankind as they are yet unknown and new.
3. The true Theory of Elasticity or Springiness, and a particular Explication thereof in several Subjects in which it is to be found: And the way of computing the velocity of Bodies moved by them.
ceiiinosssttuu
Ut tensio sic vis. (As the extension so the force.)
Hooke’s law

## Slide 8
Hooke’s law
principal stresses and strain increments:
symmetric

## Slide 9
Hooke’s law
uniaxial tension
Young’s modulus E = (P/A)/(δ/)
Poisson’s ratio ν = – (δd/d)/(δ/)
direct observation of elastic constants

## Slide 10
Hooke’s law
axial symmetry:
compliance/stiffness matrices not symmetric because stress and strain variables not work conjugate

## Slide 11
Hooke’s law
separate change of size and change of shape
work conjugate stress and strain variables
bulk modulus:
shear modulus:
change of size and change of shape uncoupled
(off-diagonal zeros)

## Slide 12
Hooke’s law
only 2 independent elastic properties for isotropic material

## Slide 13
Stiffness in conventional drained triaxial compression
total stress path in conventional compression
(constant cell pressure):

## Slide 14
Stiffness in drained triaxial compression

## Slide 15
Stiffness in undrained triaxial compression
no coupling between change of size and change of shape – compression and distortion – for isotropic elastic soil
hence, in undrained test – pure distortion – δp'=0 and pore pressure parameter a = 0 for isotropic elastic soil
conventional triaxial compression δq/δp = 3 and δu = δp = δq/3
pore pressure from total mean stress alone
effective stress path independent of total stress path

## Slide 16
Stiffness in undrained triaxial compression
in undrained test
external view of undrained stiffness in terms of total stress increments:
distortional stress q = σa – σr = σ'a – σ'r and hence Gu = G

## Slide 17
Stiffness in undrained triaxial compression
δεp = 0 (undrained)
δp arbitrary (external change of total stress)
hence Ku = 

## Slide 18
Stiffness in undrained triaxial compression
νu = 1/2
drained and undrained elastic properties cannot be chosen independently

## Slide 19
Elastic stiffness from different devices
oedometer
one dimensional compression
and Ko = ν/(1-ν)

## Slide 20
Elastic stiffness from different devices
pressuremeter
direct measurement of shear modulus G

## Slide 21
Elastic stiffness from different devices
plate loading test
composite stiffnesses do not reveal individual elastic properties

## Slide 22
elasticity
simple models assume isotropic linear elasticity
two parameters: E, ν or G, K
convenient but not necessary
explore possibility of anisotropy
and nonlinearity

## Slide 23
anisotropic elasticity
many soils deposited over areas of large lateral extent
implied symmetry: all horizontal directions equivalent: B, C, D, E
cross anisotropy – transverse isotropy
(anisotropy of real soils, after real stress/strain histories will be more complex)

## Slide 24
different modes of shearing
cross anisotropy
5 elastic properties
triaxial can only find 3: Ev, νvh, Eh/(1-νhh)
νhh? Gvh? could use bender elements

## Slide 25
Graham & Houlsby 3 parameter cross anisotropy
axisymmetric triaxial conditions
coupling of compression and distortion

## Slide 26
Graham & Houlsby 3 parameter cross anisotropy
axisymmetric triaxial conditions
forcing particular link between cross anisotropic elastic parameters
coupling of compression and distortion

## Slide 27
effective stress path in undrained triaxial compression
α2 = 1.52 = Eh/Ev
Winnipeg clay (Graham & Houlsby)

## Slide 28
experimental techniques
laboratory geophysics
bender elements
shear wave velocities: time, distance
Vvh = Vhv ? (elastic, symmetry)

## Slide 29
alternatively:
small undrained unload-reload cycles during drained test
slope of effective stress path indicates elastic anisotropy
vertical Eh = Ev, α = 1
anisotropy evolves with stress ratio
Eh  0 at critical state
Hostun sand (Gajo)

## Slide 30
Gault clay
evidence of stiffness anisotropy from bender elements
Gault clay and Hostun sand
evolution of elastic anisotropy with stress ratio

## Slide 31
cross anisotropy – axis of symmetry of anisotropy coincides with vertical axis of sample
more general anisotropy – misalignment of axes – sample distressed – boundary measurements may be unrepresentative
it is tempting to assume that things that you choose not to observe do not exist

## Slide 32
empirical description of elastic nonlinearity or evolution of anisotropy
hypoelasticity
not necessarily conservative – energy production/dissipation in closed cycles
for example, both G and K functions only of p'
hyperelasticity
thermodynamically consistent
define strain energy density function U
or complementary energy V
hence stiffnesses

## Slide 33
complementary energy function (Boyce, 1980)
constant volume paths
constant distortional strain paths
road sub-base material: n = 0.2, ν = 0.3 (K1/G1 = 2.17)

## Slide 34
Boyce complementary energy function
contours of constant volumetric strain and constant distortional strain

## Slide 35
Cam clay has K dependent on p'
constant ν is thermodynamically unacceptable
Houlsby strain energy function
constant distortional strain paths: η = constant
constant volume paths
asymptotic to

## Slide 36
Houlsby strain energy function
contours of constant volumetric strain and constant distortional strain

## Slide 37
art in choosing energy functions to give desirable properties when differentiated twice (stiffness or compliance)
varying slope of undrained path may come from nonlinearity or evolving anisotropy (or both)
subtle tests to distinguish
even more difficult to discover hyperelastic energy functions to describe evolving elastic anisotropy
nonlinear elasticity – or plasticity? (irrecoverable strains)

## Slide 38: Summary
generalised Hooke’s law – one-to-one link between stress and strain
elastic matrices symmetric with work-conjugate variables
two independent elastic properties for isotropic material
deduction of elastic properties from standard tests
evolving anisotropy - nonlinearity