Geotechnical  Engineering, Vol.  6, 1975

A CRITICAL RE-APPRAISAL OF THE INCREMENTAL STRESS-STRAIN THEORY FOR  NORMALLY CONSOLIDATED . CLAYS

A.S. BALASUBRAMANIAM*

SYNOPSIS

The incremental stress-strain  theory of RoscoE & PooROOSHASB (1963) is presented (in a slightly different form) with respect to shear strains.   A comprehensive series of stress-con trolled triaxial tests was carried  out  and  the results  were compared  with the predictions of the theory.  The stress ratio-shear strain relationship of normally consolidated specimens sheared under undrained  condition  was unique and was independent of the consolidation pressure.  Als.o, provided that the effect of the initial one-dimensional conso'lidation stress is

absent, the state boundary surface is unique for all types of tests including anisotropic con-

solidation.   During anisotropic consolidation, the strain increment ratio was a constant and the void ratio varied linearly with the logarithm of the mean normal stress (the slope of the line is the same as that for isotropic consolidation).   The volumetric strains in all typs of tests on normally consolidated clays may be successfully predicted from the state boundary surface as obtained  from  undrained  tests.   However, the shear strains  may only  be pre dicted for paths in which the stress ratio increases or remains constant.

INTROPUCTION

This  paper  is concerned  with  a  critical  re-appraisal   of  the  incremental stress-strain theory for normally consolidated clays developed by RoscoE & PooROOSHASB (1963).  The basic assumptions made in the theory are examin ed, and the predictions from the theory are compared  with experimental  ob servations from a large number of stress controlled triaxial  tests in which the specimens were subject.ed to a variety of applied stress paths.

Several stress-strain  theories have recently been developed to describe the stress-strain  behaviour  of  normally  consolidated  clays;  see RoscoE, ScHo FIELD & THURAIRAJAH (1963), ROSCOE & BURLAND (1968) and  SCHOFIELD & WROTH (1968).   In  these theories,  a fully saturated   normally  consolidated clay is assumed to behave as an elastic-plastic material.  Based on this assump tiop, concepts such as yield surface and normality were used to obtain an ex pression for the strain increment ratio in terms of the stresses.  · This expres sion was combined with an independent  relationship for the strain  increment ratio  obtained,  from  an  energy  balance  equation.     Thus,  a  stress-strain

*Associate Professor of Geotechnical Engineering, Asian Institute of Technology, Bangkok, Thailand.

Discussion on this paper is open until 1 May 1976.

A.S. BALASUBRAMANIAM

theory for the prediction of strains in normally consolidated  clays was deve loped.    BALASUBRAMANIAM (1969), has shown  that  for  stress  paths  with in creasing stress ratios these theories which are based on some of the concepts of plasticity theory and on an energy equation  are  mathematically  similar (and in some case identical)  to the incremental  stress-strain  theory  of RoscoE  & POOROOSHASB (1963).  It therefore appears that the ROSCOE & POOROOSHASB's theory is more fundamental  and should be examined critically for its precise validity.

In deriving the incremental  stress-strain  theory,  RoscoE  & PooROOSHASB (1963) assumed  a unique state  boundary  surface for  normally  consolidated clays.   The state boundary  surface in the p, q, e space (where p is the mean normal stress, q is the deviator stress and e is the void ratio) is a surface con fining a space between itself and the origin within which a point can represent a state of an element of soil, but  outside  of which a point  cannot  represent such  a  state.    The  uniqueness  of  the  state  boundary  surface  will also  be examined.

Experimental evidence will be presented  to illustrate that the  state  path followed during  anisotropic  consolidation   (i.e. consolidation   with constant stress ratio) does lie on the state  boundary  surface obtained  from undrained stress paths.  The variation of strains and void ratios during anisotropic consolidation will also be studied.   Finally, for the prediction  of strains, the basic hypothesis that any applied  stress path  on  the  state  boundary  surface can  be considered  as an infinite number  of small steps of undrained  stress paths and anisotropic  consolidation  paths, will be examined for a large variety of applied stress paths.

Stress  and Strain Parameters

The stress  parameters  used  in the analysis of triaxial test results are :

p  =  (cr/  + 2cr/)/3 and 	q  =  (cr1'- cr3')

(Note that in the triaxial test cr2 ' = cr/)

where cr 1' , cr2 ' and cr/  are  the  principal  effective compressive stresses.    In terms  of the  principal  compressive  strains,  E 1, E2  and E 3,  the relevant strain parameters for use under the axi-symmetric conditions of the triaxial test (E2  = E3)  are :

V  =  (E1 + 2 E3)

and 	E  =  2(E 1 - E3)/3,

16

INCREMENTAL STRESS STRAIN THEORY

The axial strain E1 is. defined as :

Lo

I

e, 	log (L./L) (Co.n;;pression being positive)

L

is the initial height and L, the current height.

L

0

The volumetric strain v is given by :

Vo

v =  IVdV

= ·1og

( V0   ) (Compressi•On bem.

g posi.ti.ve)

v	.

V0   is the initial  volume and  V, the current  volume.	Expressed in terms of void ratios·(e)

v  =  log

1 + eo  )

(

l+e

-

where e0  is the void ratio of the sample at the end of isotropic consolidation.

In this paper, unless otherwise stated, v and E will be measured from the state

of the sample under isotropic stress conditions and just prior to shear.

MATERIAL  TESTED,  SAMPLE  PREPARATION  AND  TESTING   PROCEDURE

All specimens were prepared from air-dried Kao.lin (liquid limit 74%, plas tic limit 42%, and specific gravity 2.6) mixed with water to a slurry of 160% moisture contenL   The slurry was one dimensionally consolidated in a spec ial mold to a maximum pressure of 22.6 lbjin2•     Subsequently, the mold  was removed and the sample was isotropically  consolidated  to  the required cell pressure.   For a detailed description of sample preparation  and testing pro cedure, see BALASUBRAMANIAM (1969).  In order to r duce  the effects of non uniformity in deformation  of the samples special precautions  were taken  by the use of lubricated  ends (RowE & BARDEN,  1964).  Leakage was virtually eliminated by employing silicon oil TING, 1968).

THESTATEBOUNDARYSURFACE

RoscoE, SCHOFIELD & WROTH (1958) put forward the existence of a unique surface in the three dimensional space relating the void ratio, e, and the stress parameters, q and p.   Two different and distinct surface could  be obtained, VIZ.   one  for  normally  or  lightly  overconsolidated  clays  and  another  one

p

Q

Isotropic Consolidation Line

State  Bol.fldory  Surface  lor

Norrndly   Coii$Oiidoted Cloys

c

for heavily overconsolidated clays. Figure 1 shows these surfaces in an isometric view. The curved surface ABCD  corresponds   to  the  state paths  which are followed by nor mally 	consolidated   specimens  in the (p,q,e) space. AB corresponds to  the  isotropic consolidation  line and  CD is called the critical state line. Specimens reaching the critical state  are assumed to have unlimit ed  shear  distortion   without 	 any change in stresses or volume. 	The ruled surface CDEF represents the failure surface of overconsolidated samples. The peak stress conditions for  a  large  number   of  normally

Fig.1. State  boundary surfaces for normally and overconsolidated clays in { p,e, q) space.

and overconsolidated specimens of Kaolin were presented by JAMES  & BALASUBRAMANIAM (1971a and b).

The surfaces ABCD and CDEF are called the state boundary surfaces.   It is·difficult to visualise whether the state paths followed by a normally conso lidated specimen lie on the curved surface ABCD. in the three dimensional plot.   Therefore, RoscoE & PooRooSHA.SB (1963), devised a method to repre sent the curved surface ABCD by a curve in a two dimensional plot.   Sub sequent, workers (see, BuRLAND, 1965) have used alternative parameters such as qfpe, and PIPe for the two-dimensional representation of the state boundary

surface.   The parameter Pe is defined as :

Pe=Poexp (eoA-, e)

.................... (!)

where e0, Po correspond to the void ratio and the mean normal stress on the isotropic consolidation line.   A. is the slope of the isotropic consolidation line on an (e, logp) plot.  Pe is called the mean equivalent pressure and  is similar to the preconsolidation pressure defined by HvokSLEV (1937).

'

RoscoE & POOROOSHASB (1963), assumed a unique state boundary surface

in the derivation of the incremental stress-strain theory for normally consoli dated clays. However, the experimental data presented by RoscoE & THuRAI RAJAH (1964), showed that  the state boundary surfaces are distinct  and  dif ferent for undrained and fully drained triaxial tests on normally consolidated

INCREMENTAL STRESS STRAIN THEORY

specimens of Kaolin. 	Also, the state paths followed during anisotropic con solidation (i.e. consolidation with constant  stress ratio) were found  to deviate from  the state  boundary  surfaces for  undrained  and  drained  test  specimens. BALASUBRAMANIAM (1974), made a detailed  study of the effects of stress his tory and other factors on the state boundary surface for normally consolidated clays.	According  to  this  study, provided  the  effects of initial  one-dimen

sional consolidation stress have not been there,  then  the  state  boundary   surface is  unique   and   is  independent   of   the applied stress paths.

Figure  2  illustrates   the  state   paths

0.6

0.4

0 0

----i--	4 'xQ------   -

-	0

I	w

followed  by  three  specimens  (T     AO    '

3 ,

rr

and   AD)    sheared   from   an  isotropic

consolidation pressure of 90 lbjin2. Specimen T3 was sheared under un drained  conditions,  specimen AO under

0.2 1-----	-----·---r - 	--

)<ey: 	j	0

X  AO 	I

constant-p-conditions and specimen AD under  fully  drained   conditions.    The state paths followed by all three speci mens are found to be approximately unique.

00..4.:----;:o_ 6-;::::--0-.81.;::---1.0

P /Pe

Fig. 2. State paths  followed  by three specimens sheared under un drained, constant  p and fully drained  conditions.

STRESS-STRAIN BEHAVIOR UNDER UNDRAINED  CONDITIONS

Undrained tests were carried out on specimens of kaolin one-dimensionally consolidated to 22 lb jin2  and  subsequently  isotropically  consolidated to  30,

60 and 90 lbjin2.    The (qjp, E)  characteristics of these specimens as shown in

Fig. 3, are found  to  be unique.    These  observations are in  agreement  with those of RoscoE & PooROOSHASB (1963) and hence the shear strain  during un drained  tests may be expressed as:

r

(o)und<ained = 	f, (n) dn	......... ... . ....(2)

BALASUBRAMANIAM (1973) has already  made a detailed  study of the effects of stress  history  on  the stress-strain  behaviour  of  remoulded  specimens  of Kaolin  tested  in the conventional triaxial  apparatus under  stress-controlled conditions.   The parameters considered  were the initial one-dimensional con solidation  pressure used in preparing the samples, the load increment,  the magnitude  of isotropic  consolidation stress  prior  to  shear  and  the type of applied stress path.    These results indicated  that  the  stress-strain behaviour under  undrained  conditions  was unique and independent  of the  initial  one-

19

dimensional stress used during sample preparation.   Load  increment size and the magnitude of isotropic consolidation pressure  prior  to shear  did not  have any effect on the (qjp, c:) relationship for  undrained tests.

0.

'0-'

0.6

i	I

--l- - ----,- --------,

I	,tr ol	Isotropic

.Q

a0::	X

Test   designation

I

rl.

22

60

lr ..	.

I - 0  stress,psi	stress,psi

IJ) IJ)

...

4>

0.4

6X--fr)-(--<:):(.  T:   · -	22 	30

ij)

i

I

o----o---o T31

----2+2  --- 90

! -- ----·--- --  I

.	I

Ir

ij'"'"                _

i i I I

I

0

2 	8	10	12	14

Shear   Strain, €,%

Fig. 3. (q/ p, c) relationship for specimens sheared under undrained condition.

ANISOTROPIC CONSOLIDATION

During anisotropic consolidation, the  stress  ratio,   cr / /cr 3'   is  maintained constant  (cr/   is the  major  principal stress  and  cr3'   is the  minor  principal q	stress).   Figure  4  illustrates a  possible experimental procedure for  such  a test

in the ( q ,p ) plot.  A specin1en is sheared under   undrained  condition  from   the

Anisotropic

Consolidation

Path 	\

I

8

Undrained

Stress Path

normally   consolidated  state   under   a cell pressure  Po corresponding to  point A.  The undrained stress path  is denot ed by AB.  From  B, the specin1en is subjected  to anisotropic consolidation along the path  BB'.  During anisotropic

consolidation  q jp  (= 11) is  maintained

"'-----'- - -	-    --'A'-----p

Fig. 4. Anisotropic  consolidation  path.

constant :

(k - 1)

11  = 3 (k + 1)

.. .... . ....... . .. . ....... (3)

where

............................. (4)

INCREMENTAL STRESS STRAIN THEORY

Figure 5 illustrates  the state  boundary  surface for  normally consolidated clays i11 the (p, q, e) space. In this figure the curve AA' corresponds to isotro pic consolidation,  while the curves BB', CC';  etc. correspond to anisotropic consolidation.    ABCD,  A'B'C'D' are constant voh!me (or undrained stress) paths.   In  this figure be'  corresponds  to  a  fully  drained  stress  path  with constant cell pressure.   It is split into two parts viz. be, an undrained stress path and cc', an anisotropic consolidation path.

q

o'

Critical  State

Line

Isotropic

Consolidation	-----.

Line	Anisotropic

.---\--:r- Consolidation

Lines

'-----Undrained	e

Stress Path

Fig. 5. Isometric  view of the state  boundary surface for normally consolidated clay.

Experimental Observations  on Anisotropic  Consolidation Tests

Altogether  five anisotropic  consolidation  tests were performed  on  speci mens initially one-dimensionally consolidated  to 22 lb/in2,  and subsequently isotropically consolidated to 90 lbjin2.    They were then sheared either under undrained condition or under constant dqjdp condition  to the required stress ratios.  The tests were designated by BF, BC, BT, BLand T10, and they cor responded to qjp (= 11)-values of0.205, 0.405, 0.51 , 0.57, and 0.71 respective ly.  The strain paths followed by these specimens in the (v, c) space are shown in Fig. 6, where the strain paths are found to be linear.   These results confirm the  original  findings of  RoscoE &  PooROOSHASB (1963), i.e.  that  (dv/dc)11

during anisotropic consolidation is only dependent  on the value of 11·	The

values of (dvjd c)11 observed for the five tests are 2.80, 1.30, 1.00, 0.775 and

0.45.  These values correspond to q jp (= 11)-values of0.205, 0.405, 0.51, 0.57

and 0.71 respectively.	Figure  7 illustrates  the variation  of (dv/d c)11 with 11

21

A.S. BALASUBRAMANIAM

for all the five tests conducted. It can be seen that  (dv jd e)11 varies uniformly with 11  and may expressed  as :

(dvjd e)11   = f2 (11)

(5)

I	I

i

\	,	I 	I

8C	-r.:,'4

-··-\- !	Test  OesionoUbn

: 	!

!

>	\   I 	I 	C>	8F

0	\ !	•	o 	ec

4 	3	-··-- -\!---------·-- ----- 	X	BT  ---·

I

'1..	! 	0	BL

0	I \ 	:	+ 	T10

__L_\

_;_

_ ! 	_       _j

- ---

2 	4 	6

.12  %

Fig. 6. Strain  paths followed by specimens during anisotropic consolidation.

1	'\ i	I	.

--·t---··:-- x,	---·-+-······-

: 	I 	.

'-+. 	I

' -....1.

Stress   Rotio, q/p

Fig. 7. Relationship between strain incre

ment ratio and stress ratio.

The changes in void ratio with the logarithm of the mean  normal stress during anisotropic consolidation on  two  specimens  (at 11  values of 0.405, and 0.57) are shown  in Fig. 8.   The variation in  e with log pis found to be linear  and

the slopes (equals to 0.26 approximately) of these lines are the same as that  of

1.24

Mean Normal Stress,p, lb/ir- 2

60     80   100 	200

Mean Nonnol Stress,p,lb/in 2

100 	150    200

1.15

1.20

.e	.

0	.2

a:   1.16

--o	-c

1.12

0.85L-----'---'----'

1\  =    o.•

>.	..   0.

1'\.    "  0.57

Fig. 8. (e, log p) relationship during anisotropic consolidation.

the isotropic consolidation line in an (e, logp) plot. by A.	Then,  during  anisotropic consolidation:

e- ec = -A logp fpc

Let this slope be denoted

(6)

where ec, Pc corresponds to any known  void ratio  and pressure  on the  aniso tropic  consolidation line.   The stress  and state  paths  followed  by two speci mens  during  anisotropic  consolidation  are  shown  in  Fig.  9.   It is noted that the state paths during anisotropic consolidation do lie on the state boun dary surface.   These results are in agreement  with the  assun1ptions made  by RoscoE and PooROOSHASB in their incremental stress-strain theory.

.......

150 ---.,...--..,..---

IOOr------+---

o. 6r--- ---,..----,

--	'

.............

0.4t----t-  -- ."...'-.:t->  ----1

.0	c

Stress	Path	p,  lbi;n  2

(a)

150 ---..,..-- ---,.----,

Co

50 	100	150	200

2

Stress	Path	p , lb/ in

State   Path	p 1 Pe

Specimen	BC

0. 6

a

0 '---"""-----"""--

0.4 	0.6	0.8	1.0

State	Path   p /Pe

( b) 	Specimen	BL

Fig. 9. Stress and state paths followed during anisotropic consolidation.

INCREMENTAL STRESS-STRAIN THEORY OF  ROSCOE AND  POOROOSHASB

Assuming a unique (p, q, e) surface, an incremental  stress-strain theory was proposed  by RoscoE & PooROOSHASB (1963) of the form  :

23

d £ 1  =  (de)	d11   +   (d

8

)	dv 	.......... (7)

d11   v	dv 	11

where (d etfd11)v corresponds to  the  variation of £ 1 with 11  in  an  undrained test, and (d e 1/dv)11 represents the variation of £ 1 with v in a constant-11 (ani sotropic consolidation)-stress path. dv and d £ 1 are the incremental volumet ric and  axial  strains.

The incremental stress-strain theory  of RoscoE and  PooROOSHASB  in Eq. 7 will now  be presented in a slightly  different  form  as follows  :

d 8  =  (d

8

)	d11   +   (d

8

)	d v	.. .. .. .. .. (8)

d11   v	dv 	v

where instead  of using the incremental axial strain  d e1, the incremental shear strain  de will be used. 	Equation 8 can  be expressed  in the form  :

d £  =  f1

(11)  d11   +

1

-

f2 (11)

dv	. .. . .. .. .. .. (9)

where f 1(11) d11  has  been  shown  to  be equal  to  the  incremental shear  strain in an undrained test (Eq. 2, and  f2 (11) is equal  to  (dvjde)11•      Therefore, the total shear  strain in any  type  of  test  can  be obtained .by  integrating Eq.  9.

Thus:

e  =  I n f1

(11)  d11   +

In	1

dv	.. .. .... .. . . (10)

0	0	f2 (11)

-

Determination of Volumetric and Shear Strains

The  procedure adopted for  calculating  the  volumetric strain  along  any applied  stress path  is as follows.   Let  AB in Fig. 10 be the applied  stress path for  which the  volumetric strain-stress ratio  relationship is being  determined. Then the undrained stress  path  AC through the  point  A is drawn  assuming that   the  state   boundary surface  is  unique   (since  intersections of  the  state boundary surface  by planes of constant void ratios  are  similar  curves).   The path  AB is divided into a large number of small  steps,  AB1, B1B2 , B2 B3   .•.•

BnB.	Then   each  step  AB1   is  considered  in  two   parts;  AC1,    along   an

undrained  stress  path   and  C1B1,   along  an  anisotropic consolidation path

(stress  ratio  11 1). 	The   volumetric strain   experienced  by  the  specimen   at

states, B1, B2    •• .•Bn, B is denoted by vB 1

,

vB   . . . .. vB, and  the  incremental

2

volumetric strain  for  the  steps  AB  , B B 	..... Bn B by dvAB  , dvB B   .....

1 	1  2

1	1 2

dvB B·   Similar   notation is  used  for  the  shear  strain, i.e.  eB , eB	..... eB

n 	1 	2

denotes the shear  strain  at states B1, B2 . • ..Bn. The  incremental shear strain

for the steps AB  , B  B  . . ..BnB is d eAB  , d eA B  ... . deB  B·  The  notation

1 	1 	2

1 	1 2 	n

24

q

e

log p.

Fig. 10. Incremental steps in the calculation of volumetric and shear strains in drained test.

for  the  shear   strains along  the  undrained stress  path AC  for  the  states C1, C2  ..... Cn  is  Ec , Ec  ..... Ec	and   for   the   incremental shear   strains for

1	2 	3

the  steps,  AC1,  c1 c2 ..... cnc is d EAc ' dEc   c .. ... dEc   c·

1 	1  2 	n

Assuming a unique state  boundary surface, it can  be shown that :

and  since:

dvAB	dvAC	+ dvc  B

=

1 	1	1  1

dvAC 	=  0

1

dvAB	=  dvc  B

1	1  1

(11)

. . . . . . . . . . . . . . (12)

Let  ( e0 , p 0)  be the  void  ratio and  the  mean  normal stress  at  point A on  the isotropic consolidation line.     Then the  isotropic consolidation line  can  be expressed as  :

(13)

25

If Pc  PB

1	1

denote the  mean  normal stress  for states  C1 and B1 and  if eB 1 is

the  void  ratio corresponding to  the state B1, then  :

e  - eB	=  -A log  (Pc  IPs  )	....... . .. . .

0

1	1	1

(14)

Also:

vB	=dvc B	=dvAB 	=log(- 1 +eo) 	··· ·····

1	1  1	1 	1 +e

B1

(15)

Hence,  knowjng e , A, Pc 	and  PB ,  eB	can  be evaluated and therefore vB  ,

0

1 	1	1	1

dvc s

, dvAB

may  be determined.

1 1	1

Similarly, considering the state points  C2 , B2  :

eo- eB	=-A log (Pc  / pB )	· · ·· · · · · · · ··  (16)

2	2 	2

and

VB	=

1Og

1 + eo )

(

(17)

2	1 + eB2

Thus,   from Eqs.  16,  17  vB	can  be evaluated.	Then  :

2

dvB B 	=	VB   -VB

1 -   2 	2 	1

(18)

The same procedure can  be repeated to determine vB  , vB	.... vB 	and  also

3	4	n

d vB   B  ,  d vB   B	. . . . . d vB  B.	Hence,  the   volumetric strain  stress   ratio

2 	3 	3    4 	n

relationship can  be established.

The  procedure adopted for  determining the  shear  strain-stress ratio  rela

tionship will now be described.	Using  Fig.  3, the shear  strain Ec , Ec .... Ec

1	2	n

for  stress   ratios ll!' lh .... 11n can  be  obtained for  points  c1' c2 . . ..en.

Similarly, using  Fig. 7, the values of f2  (11) can be estimated for the  paths  with stress  ratios 111, 11 2 .. .. 11n.

Hence:

EB1

=  Ec1

+   f2 (111) dvA1 B2

·· · · · · · · · ·  (19)

EB	=  Ec

2	2

+  f2 (111) d vA B	+ f2 (112) dvB B	·· · · · ·  (20)

1	1  2

and                                      c:B      =  Ec  +  l: f2 (11)  dv       ... .... ....... (21)

Thus, the  shear  strain-stress ratio  relationship may  be obtained.  The  above calculations of the volumetric and shear strains are carried out by using a com puter and  taking increments of stress  ratio of 0.01 for  all applied stress  paths discussed in the subsequent section.  Any further reduction in the stress  ratio did not  have  any  appreciable effect on  the  magnitude of the strains.

COMPARISON OF OBSERVED AND  PREDICTED STRAINS FOR  A VARIETY OF STRESS  PATHS

Constant Mean Normal Stress Path

A  constant mean  normal stress  test  was  carried out   starting at  90  lbjin2

isotropic stress.    During this  test,  the  axial  stress  and  the  cell pressure were

26

90

(\j

c

so 	. .

c:

|  |  | ore_----- P | - |
| --- | --- | --- | --- |
|  |  | I I I :------ --- --- 0 Test AO l |  |
| 9 9' ttredicted _ |  |  |  |
| ! - |  |  |  |

'. 60

u

1/)

1/)

----- -----

Q.--

0/...

-c-l--_......

---

en  3o

....

0

0

-

a

q..-,9 LPredicted

,"

I

(Y

I

0 Test lAO

I

0	2 	4	6	8 	0

Volumetric Strain,  v ,%

5	10 	15	20

Shear · Strain, € , %

Fig. 11. Observed and predicted stress-strain relationships for constant p test.

adjusted, in such a way that the mean normal stress p remained constant.   The state  path followed by this specimen can be viewed in  the ( q fpe, PIPe)  plot, which has""already been presented in Fig. 2.  The (q, c:) and the (q, v ) charac teristics for this specimen are shown in Fig. 11.   In this figure, the experimen tal points  are shown  as circles and  the predictions  from  the theory  by the dotted   curve.    Excellent  agreement   between  experimental   and  predicted

strains can be observed.

Fully  Drained Stress  Path

90 ,.---,----- --, ,---  - ,-	.................

"'c	: 	I	- --/

sor-

I 	I	-r--t-..-..-

----

A fully drained test with constant

---1-----+-

1  _.,9,/	1

cell pressure was performed starting 	·	P... --P   redicr ed 	I

from 90 1b/in2  isotropic  stress con- 	. 3o r-	.J. _...... ·	!	o rest   Ao -

dition.   The state path followed by	0,9"9' / 1 	:i	jI

'	,

this specimen in the ( q fqe,PIPe) plot,

has  already  been  shown in Fig. 2.

T	i	I

0 ---2 ----4---

------

s 	a	10

The (q, c:) and the(q, v) relationships for this specimen are shown in Fig.

12.  In this figure, the experimental points  are   plotted  as  circles  and the  .predictions   from   the   theory are indicated by the dotted curve. Again good agreement is noticed between experimental and predicted strains.

Constant  Deviator  Stress  Path

Volumetric  Strain , v, %

,   0,,.,...	'

-

;

...

1	o........... j

; ...,  ·	J   Predicted - ----·---

;:!  )

d 	I

,6	i

- !---- ·

'

10 	1 5 	20

Shear Strain, €,%

The  stress  paths  considered  so  Fig. 12.

far 	were  such   that   the  deviator

Observed and predicted stress-strain relationships for fully drained test with constant cell pressure.

27

A.S.  BALASVBRAMANIAM

stress  q and  also  the  stress  ratio  q jp were   increasing.    For    a   constant q-stress path,the stress ratio decreases. The  stress  path  followed  by  a  spec imen BX is shown in Fig. 13.   In this

figure,   the   specimen    was   initially

Mean Normal Slress ,p,lb    2

/in

sheared   along   an   undrained  stress path  AB and  subsequently the devia

o.a .- --	---,.-•----.,-  -

1

!,..-- --,----,

tor  stress  q was maintained constant

I 	I

j	I

s	1	I

o.6   -,-·---L------"-· -:-'- 	,----1

along  path  BC,  while the mean  nor

mal   stress   p 	was  increased. 	The

a.	o:'I	''0.1...............	'

I	I'

/	......'tr-l_fP'@i'Cied	I

·-a	p	.   --o---L	I

a::  0.4  '----- --"-	- -------- - ==-----!.__ --·-'-.----

observed   and 	the 	predicted 	volu

metric strains  for the stress path ABC

I	I  --o---.,L---o----o--c:

0.2	-------- 	I	i	I ----1

--t----!------'--

I	i

I 	:

are  also shown  in  Fig. 13. Excellent

agreement  is  again   noted    between

·o-----

i

! -	7

i

the  two  strains. 	However, for   the

3--

Volumetric  Stroin , v ,%

s-- 6

stress paths for  which  the stress  ratio

Fig. 13. Constant q test (a)  stress path

(b) stress ratio-volumetric strain relationship.

( q jp)	decreases, 	the 	incremental

stress-strain	theory 	of 	RoscoE 	&

PooROOSHASB cannot be used for  the

prediction of  shear   strains.    For  such  paths,   the  incremental stress-strain theory  could  perhaps be modified  by neglecting the undrained component of the  shear  strain on  the  right  hand  side  of  Eq.  8.     This  would  lead  to  the

expression for  shear  strain  as  :

d £  = ( ) . dv. dv 	11

(22)

In Eq. 22, it is assun1ed that  the value

1 	Q --.,.  ,   i 	,

0.61---r---or--"·---r---r,-: --t·----

I	.........	Prtdiered

.......j	I	I  ' ,

c:r	..,.,,.·."'      .	•     0	' ,,

j  /	'

0.4 	-O,f....  -·-- i_  	;,__ .Q. 	: ·-·-   -··· ' ·-

of (de) 	which is given by 1/f2 (11), dv 	11

when  11   is   increasing is   also   valid

"'

(/)

/ !	'	! 	o	!	I ' ...,,

,' 	0  I	'

/ 	c

o/

0.2    I    -- - --- -:· --"·-·--t---:·----f

/	f	:

I

!

when 11 is decreasing.	The  observed

and the predicted strains for the stress paths  ABC  (shown   in  Fig.  13)  are

shown in Fig. 14, where the prediction

Shear  Strain I€ I/o

0

Ia 	is  somewhat  more   than   the  actual strains  for  the phase  in  which  q  was

Fig. 14. Stress  ratio-shear  strain  relationship

for constant q test. 	maintained  constant.

Reloading of Specimens with Initial States on the State Boundary Surface

The   stress-strain behaviour during subsequent unloading (deviator stress)

28

and reloading (deviator stress) of initially sheared samples with the mean normal  stress  p  increasing all the time will now be considered . The

type  of  stress  path  imposed  on  a

roo

I

I

. --+I --  ---1	I

I

I

I

1

I	I	i

sample,and its previous stress history "'  80 --	--'--·

is shown in Fig. 15. This  specimen  o-

---f- ---+--

!

1

was initially sheared from the isotro- pic stress state A to the stress state B

l

.g

"' so

iii

-----;------

i

with increasing stress ratio. 	Subse-  -

quently,  the  specimen  was sheared

from B to C along a stress path with

40	1

1- -  - sf-------   :---t--- H-	-    -l

decreasing   deviator   stress (q )  and 	20

increasing  nl.ean normal  stress ( p). 	c

This second phase of shear can be divided  into  two  types,  depending on  the  slope  of  the  applied  stress

0	A

07-- 90 ----IIL--------	----170

Mean  Normal  Stress, p, lb/in 2

path. 	In  one  case,  the stress  path  Fig. 15. Stress  path followed by Specimen BP, Showing   the   phases   in 	which	the

BC lies above the downward tangent                deviator stress was decreased and  then

to the undrained  stress path  AB at               increased.

B.  For  this case, the  point  C  will lie on  the state  boundary  surface  and, therefore,  the  specimen  will be in  a  normally  consolidated  state.    In  the second case, the stress path BC lies below the tangent to the undrained  stress path and the point C will lie below the state  boundary  surface.  Only the first

0.4	l A

!	I	,//

0 .3 -	---<- - ------- --- ---      -	--+----- -----+-	-  - --- ---,L..t-L,

1',	I	!	/

0.	I   I

,.."---1------

6-	/	I	'',, 	I	!	1,	// /	I

0	I 0 	I	I	' ........    I 	I

,<-r-	/1.	----	-·----l,,-----i

I	/ ,

o 	II

I,	v,	1	I	/

,i

Predi cted 	"	j

0

0.2 ------- ' 	- 	--1  - --------

?	i	i	'

0.1  J._ 	j_  	i------'---.

I	i

o-- --	----j -- 	-- 	----- --	--

Voiumstric  Strom •  v • %

Fig. 16.  Observed and predicted stress  ratio-volumetric strain  relationship  for the specimen subjected  to stress path shown in Fig. 15.

A.S. BALASUBRAMANAIM

type of  stress  path  during  which the state of the sample always lies on  the state  boundary  surface  will be considered  for  the  phase BC.    In  the  third phase  of  shear  (CD),  the  specimen  was  subjected  to  a  stress  path   with increasing stress ratio.     The observed and  the  predicted  volumetric  strains for  the  path  ABCD  are  shown  in  Fig.  16.  Excellent  agreement  is  noted between observation  and  prediction  for all three phases of shear, i.e. AB, BC and CD.  The shear strain  experienced  by  the  specimen during the loading and   the  reloading   phases   (i.e. AB  and  CD) is shown in  Fig. 17.  In  this figure,  the  predicted  and  observed  values of  the  shear  strains  have  been made to coincide at point C (which is the start of the reloading phase).  This procedure  is  adopted, since it  has  already  been  shown  that  there  is  very little agreement  between  observed  and predicted  shear  strain  for  the  phase in which the stress ratio is decreasing. Good agreement.is noted, however, between observed and  predicted shear strains for the reloading phase CD.

0.5 ,-----,..----r---.---r----.---,L -:;:: >--o·-1.---,

D

I	1 	./o1

I	/ --/

·--;----- ;-   . ---·------	l p--"	-'----- -- .  -----··;--- -----

'	!I	.-"--·r	.

I	./ 0 	' 	/	I	.

PrediCTed 7"-----1-,---- ,,1   ' --

.

Pre--d1e-ted......  -  ....  ----  --·-·-- ---

.2 	_/r	·	/ :	·	·

I  J	l	p  I

0

a: 	-/) -- ....    j    - t----l---  	l 	--1-----------·!-.. -------+---·--·-

1	!	I 	I	I	:	i 	I

o/ 	!	!   o,'	:

/	: 	I

/ --!-..	!0 !

I	I

6	i

I

I

---,-----i·--t---r-I  ·---,---!------

A

·o 	2 	3	4 	5 	6	7

Shear   Stroin I eI%

Fig. 17.  Observed and predicted stress ratio-shear strain relationship for the specimen subjected  to stress path shown in Fig. 15.

CONCLUSIONS

A critical reappraisal of the incremental  stress-strain  theory of  RoscoE & PooROOSHASB has been made.   From  experimental  observations  and predic tions the following conclusions are reached:

(1)   The (qjp, E) characteristics  of normally consolidated specimens sheared under undrained conditions are unique and independent of the con solidation  pressure.

(2)   Provided  that  the effect of the initial one-dimensional consolidation stress is absent,  the state  boundary  surface is unique for  all types of tests on a normally consolidated  clay.

(3)	During anisotropic consolidation,  the strain  increment  ratio  (d vjdc:)11

is a constant.

(4)   During  anisotropic consolidation,  the void ratio  varies linearly  with the logarithm  of the mean normal stress.  The slope of the line is the same as the slope 'A of the isotropic consolidation  line in an (e, og p) plot.

(5) 	The state path during anisotropic consolidation lies on the state boun

dary surface.

(6)   The volumetric strains in all types of tests may be successfully predict ed from the state boundary  surface for normally  consolidated  clays as obtained  from undrained  tests (or  other  types of tests), provided  that the states of the sample lie on the state  boundary  surface.

(7)   The shear  strain  in all types of tests on normally  consolidated clays may be predicted from  the incremental stress-strain  theory  of RoscoE

& PooRoos:HASB, provided that the stress paths are such that the stress

ratio always increases or  remains constant.

ACKNOWLEDGEMENTS

The experimental  work presented in this paper was carried out in the Engi neering Laboratories at the University of Cambridge.    The author  wishes to thank his supervisor, Dr. R.G. James and the late Prof. K.H. Roscoe for their unstinted help and valuable guidance.   The manuscript  of this paper was pre pared at the Asian Institute of Technology.  Thanks are due to Prof. Za-Chieh Moh, Prof.  Edward  W. Brand,  Dr. Peter Brenner and  Mrs. Vatinee Chern.

REFERENCES

BALASUBRAMANIAM, A.S. (1969), Some Factors  Influencing the Stress-Strain  Beha

viour of Clays, Ph.D. Thesis, Cambridge University,  England.

BALASUBRAMANIAM, A.S. (1973), Stress History Effects on Stress-Strain Behaviour of a Saturated Clay, Geotechnical Engineering, Vol. 4, pp. 91-111.

BALASUBRAMANIAM, A.S. (1974), A Critical Study of the Uniqueness of State Bounda

ry Surface for Saturated Specimens of Kaolin, Geotechnical Engineering, Vol. 5, pp.

21-3S.

JAMES, R.G. and BALASUBRAMANIAM, A.S. (1971a), The peak Stress Envelopes and their Relation to the Critical State Line for a Saturated Clay, Proc.4th Asian Regional Conf  Soil Mech. Found. Eng., Bangkok,  Vol. 1, pp. 115-120.

JAMES, R.G. and BALASUBRAMANIAM, A.S. (1971b), A Comprehensive Experimen tal Study of the Strength  Characteristics of Remoulded Specimens of Kaolin,  Geo technical Engineering, Vol. 2, pp. 21-33.

A.S.  BALASUBRAMANIAM

HVORSLEV, M.J. (1973), Uber  die Festigkeitseigenschaften Gestorter Bindiger  Boden,

Thesis, lngeniorvidenskabelige, Skrifter, Series A, No. 45.

ROSCOE, K.H. and BURLAND, J.B. (1968), On the Generalised Stress-Strain Behaviour of Wet Clay, Engineering Plasticity, Cambridge University Press, 1968, pp. 535-609. ROSCOE, K.H. and POOROOSHASB, H.B. (1963), A Theoretical and Experimental Study

of Strains in Triaxial Tests on Normally  Consolidated Clays, Geotechnique, Vol. 13,

pp. 12-38.

ROSCOE,   K.H., SCHOFIELD, A.N.  and   THURAIRAJAH, A.  (1963),  Yielding  of

Clays in States  Water than Critical, Geotechnique, Vol. 13, pp. 211-240.

ROSCOE,  K.H., SCHOFIELD, A.N. and WROTH, C.P. (1958), Yielding of Soils. Ceo

technique, Vol. 8, pp. 22-52.

ROSCOE,  K.H. and THURAIRAJAH, A. (1964), On the Uniqueness of  Yield Surfaces for Wet Clays, Proc. Int. Symp. Rheology and Soil  Mech., IUTAM- Grenoble, pp.

364-381.

ROWE, P.W. and BARDEN, L. (1964), The Importance of Free Ends in the Triaxial Tests,

Journal Soil Mech. Found. Div., ASCE, Vol. 90, SM. 1, pp. 1-27.

SCHOFIELD, A.N. and WROTH, C.P. (1968), Critical State  Soil  Mechanics, McGraw Hill, London.

TING, W.H.  (1968), Some Effects of History  on the Stress-Strain Behaviour   of Kaolin,

Ph.D. Thesis, Cambridge  University, England.

APPENDIX : NOTATION

e

eo - f1,fi - k

L Lo p- Po Pe

q-

v-

V

V0  -

voids ratio

voids ratio prior to shear functions

principal effective stress ratio cr / /cr/

current height of sample initial height of sample mean normal stress

mean normal stress prior to shear mean equivalent pressure

deviator stress volumetric strain

current volume of sample

initial volume of sample

cr1',  cr2·', cr/- principal effective compressive stress. c:1,  c:2 , c:3  -	principal compressive strains

€  -	shear strain

'A

ll -

slope of isotropic consolidation  line in (e, log p) plot

qjp